## Slide 1
Quantitative modelling of electron transport using DFT
Ivan Rungger, Maria Stamenova, Andrea Droghetti and Stefano Sanvito
School of Physics and CRANN, Trinity College Dublin, IRELAND
Sao Paulo, Brazil October 2014
Notes: 1

## Slide 2: Outline
Lecture 1: Practical introduction to quantum transport
  Why is it important?
  From simple models to NEGF
  Inelastic scattering within NEGF
Lecture 2: Is DFT-transport predictive?
  DFT based electron transport
  Problems with DFT for transport through molecules
  Master equation approach
Lecture 3: Solid state spin-electronics devices
  Magnetoresistance in magnetic tunnel junctions
  Spin transfer torque
  Strong correlations: Kondo effect
Notes: 2
Mention: “is it predictive”: once we know all atomic positions, can we predict the transport properties?

## Slide 3: Why magnetic tunnel junctions?
Notes: 3

## Slide 4: Why is it useful ?
From Wikipedia
Hard-disk technology

## Slide 6
Parallel
Anti-Parallel
MR =
I
P
I
AP
I
AP
Magnetoresistance
Notes: Mention that part of difference between theory and exp is due to defects

## Slide 8: Simple theory of tunneling
Notes: 8

## Slide 9
Basic tunneling

## Slide 10
Translational invariance
kz
ky

## Slide 11: kx-ky dependent transmission
kz
ky
kz
ky
T small
T large
kx
ky
Notes: 11

## Slide 12: Spinpolarized electrodes: 2 spin-fluids model
EF
E
DOS
Majority 
Minority 
Notes: 12

## Slide 13: Fe/MgO/Fe tunnel junctions
Notes: 13

## Slide 14
Parallel
Anti-Parallel
MR =
I
P
I
AP
I
AP
S. S. P. Parkin et al., Nature Materials. 3, 862 (2004)
Tunneling magneto-resistance (TMR)
W.H. Butler et al., PRB 63, 054416 (2001)
Theoretical prediction:
Notes: Mention that part of difference between theory and exp is due to defects

## Slide 15
Parallel
Anti-Parallel
Resistance and TMR
Yuasa et al., Nature Materials 3, 868 (2004)
IAP
Resistance increases exponentially with the thickness with a damping coefficient α
IP
RA (Ωμm2)
MR ratio (%)
tMgO (nm)
tMgO (nm)

## Slide 16
S. Yuasa and D.D. Djayaprawira , J. Phys. D: Appl. Phys. 40, R337 (2007)

## Slide 17
TMR versus bias voltage
Can we describe the I-V and TMR-V with ab initio methods?
What is the origin of the decay of the TMR with increasing bias?
Yuasa et al., Nature Materials 3, 868 (2004)
Normalized MR
Bias V (mV)

## Slide 18
Band structures
Fe
MgO

## Slide 19: Why Large TMR?
A. V. Khvalkovskiy et al., J. Phys. D: Appl. Phys. 46, 074001(2013)
W. H. Butler et al., PRB. 63, 054416 (2001)
Notes: 19

## Slide 20: Why the large TMR? Fe/MgO is a “half metal”
Fe
MgO
W.H. Butler et al., PRB 63, 054416 (2001)
Notes: 20

## Slide 21: Why the large TMR?
FM1
FM1
MgO
Notes: 21
Mention: high spin-polarization of current leads to large MR

## Slide 22
E-EF (eV)
2
1
0
-1
-2
Zero-bias transmission
states in the electrodes
interface states

## Slide 23: Comparison to experiment
4 MgO layers: TMR = 1700 %
for thicker junctions (16-24 MgO layers) : TMR = 30000 - 40000 %
experiment : TMR < 1100 %
Notes: 23

## Slide 24
Bias dependence

## Slide 25
Charging and potential drop

## Slide 26: Current versus voltage
Parallel
Anti-Parallel
Notes: 26

## Slide 27: Why does TMR decay with bias?
4 MgO layers
8 MgO layers
Rungger et al., PRB 79, 094414 (2009)
Rungger et al., JMMM 316, 481 (2007)
For larger bias Δ1 states are found also in the minority spins, so that the minority current increases
TMR decreases
Yuasa et al., Nature Materials 3, 868 (2004)
Experiment
Bias V (mV)
Notes: 27
Say: investigated by a number of groups, we all came to same conclusions

## Slide 28
Oxygen vacancies
MgO band structure with Oxygen vacancy (1/16)
Defect band with band center about 1 eV below the Fe Fermi energy
0-bias transmission for an 8 ML junction, and for a vacancy in different positions
For P alignment the transmission is almost not affected
For AP alignment the transmission increases as the vacancy gets closer to the interface. The reason is an increase of the Δ1 DOS in the minority spin
parallel
anti-parallel

## Slide 29: TMR versus bias
Structure of the interface is key
Theory can match quantitatively experiment if disorder/defects are taken into account
I. Rungger et al., to appear in book chapter (Spin Transfer Torque Memory) in “Nanomagnetic and Spintronic Devices for Energy Efficient Memory and Computing, Wiley.
Notes: 29
SAY: quantitative predictions if experimental structures are used
Say: how can we know the right structure if everythiong is buried?
AP current is strongly enhanced by oxygen vacancies, especially if they are close to the interface, leading to a reduction of the TMR
These type of defects close to the Fe/MgO interface lead to a depolarization of the Δ1 DOS, thereby reducing the TMR
High quality interfaces are needed in order to obtain high TMR values
Theory can match quantitatively experiment if disorder is taken into account

## Slide 30: Spin Transfer Torque
Notes: 30

## Slide 31
MRAM (magnetic random access memories)
How can we switch the free layer?
Current induced spin transfer torque

## Slide 32
Spin Transfer Torque
Notes: Mention
that out of plane torque is non zero also at 0 bias

## Slide 33
Title
Spin Transfer Torque
Conservation of momentum leads to spin transfer torque

## Slide 34
Spin Transfer Torque

## Slide 35
DFT with non-collinear spins

## Slide 36
Spin Transfer Torque
SubSystem 1 (SS1)
SubSystem 2 (SS1)

## Slide 37
STT for Fe/MgO/Fe
x
z
V=0.5 Volt

## Slide 38
Spin Transfer Torque on right Fe electrode
In plane torque
Out of plane torque

## Slide 39
Spin Transfer Torque

## Slide 40
Spin Transfer Torque
Landau-Lifschitz-Gilbert equation

## Slide 41
Spin Transfer Torque
P to AP switch (V=0.3 Volt)
AP to P switch (V=-0.4 Volt)

## Slide 42
Towards industrial needs…
Write error rate is critical parameter

## Slide 43: Correlated linear response transport in nanostructures
Notes: 43

## Slide 44
The algorithm
Correlated impurities
N. S. Wingreen and Y. Meir, PRB 49, 11040 (1994)
Y. Meir and N. S. Wingreen, PRL 68, 2512 (1992)
Can be described within NEGF by adding an additional self-energy

## Slide 45
The algorithm
G. D. Scott and D. Natelson, ACS Nano 4, 3560 (2010)
Experiment
Kondo effect: experiments

## Slide 46
The theoretical model
How to get the many body self-energy?
Correlated atom
D. Jacob et al., PRL 103, 016803 (2009)

## Slide 47
The theoretical model
How to get the many body self-energy?
Correlated atom
Impurity solver
Impurity solvers:
Non-crossing approximation
One-crossing approximation
FLEX
Continuous time quantum Monte Carlo
Project full system on correlated atom
0
d
d
D. Jacob et al., PRL 103, 016803 (2009)

## Slide 48
The theoretical model
Current
Meir-Wingreen...

## Slide 49
The theoretical model
Neglect incoherent contributions
Landauer...

## Slide 50
The algorithm
D. Jacob et al., PRL 103, 016803 (2009)
DFT based calculations
Kondo effect

## Slide 51
Continuous-time
quantum Monte Carlo
(interaction/hybridization expansion)
Stochastic optimization
A.S. Mishchenko et al., PRB
62, 6317 (2000)
Analytic continuation
E. Gull, A. J. Millis, A. I. Lichtenstein, A. N. Rubtsov, M. Troyer, P. Werner, Rev. Mod. Phys. 83, 349 (2011)
The theoretical model
Continuous time quantum Monte Carlo

## Slide 52
The algorithm
U= 2 eV, T= 50 K
d
d = 3.8 Ang
d = 4.2 Ang
Example system
In DFT: Au chain test sytem

## Slide 53
2D Topological insulators – Kane&Mele model
.
C.L. Kane and E.J. Mele, Phys. Rev. Lett., 95, 146802 (2005)
(convetion: energy in units of t, t = 1 in this talk)
Notes: 5353

## Slide 54
2D Topological insulators – Kane&Mele model
.
C.L. Kane and E.J. Mele, Phys. Rev. Lett., 95, 146802 (2005)
T =2 (1 for each edge)
k
Notes: 5454

## Slide 55
Topologically protected states: 1D scattering
No back scattering
t
r
Notes: 55
Mention:
->Overall the spin-polarization is 0, however due to spin-orbit interaction the band structure is different for up- and down-spins ()
-> We are going to show experiments where this has indeed been shown for step-like potentials, and then our ab initio calculations for that
->The two spin channels are independent:no back scattering possible, therefore transmission is perfect

## Slide 56
.
2D Topological insulators – Kane&Mele model
Magnetic impurity on the edge
- Local moment
- Broken time-reversal symmetry
- Conductance can drop
Notes: 5656

## Slide 57
Transport direction
Correlated
substitutional impurity
Kane&Mele model: correlated impurity
Notes: 5757

## Slide 58
The algorithm
Kane&Mele model: correlated impurity

## Slide 59
No magnetic impurity
Notes: 5959

## Slide 60: Coherent transmission
Local moment regime
T=0.2
T=0.01
T=0.5
Coherent transmission
Coherent transmission
Kondo regime
High temperature regime
In the Kondo regime:
No impurity induced scattering within linear response
Notes: 60
yyy: what is our value of U (4 ?)?
Yyy: remove self-energy curves? Mayve just mention that self-energy vanishes

## Slide 61
Kondo screening
J. Maciejko et al. Phys. Rev. Lett. 102, 256803 (2009)
F. Goth et al., Phys. Rev. B 88, 075110 (2013)
F.M. Hu et al., Phys. Rev. B 88, 045106 (2013)